Supplementary information

Table SI. Table summarizing the standards used for the assessment of solubility, disintegration and water sorption.

| Standard | Definition | Requirements recommendation | Test Requirements |
| --- | --- | --- | --- |
| International Organization for Standardization (ISO) 6876:2012 [17] (Used for root canal sealing materials) | Solubility calculated as a difference in the mass of the petri dish as a percentage of the original combined mass of the specimen | Solubility value should not exceed 3% by mass. In addition, there should be no visible sign of disintegration in the specimen | Cylindrical specimens, 1.5 mm ± 0.1 mm thickness, and 20 mm internal diameter Samples immersed in distilled water for 24 h |
| American National Standards Institute (ANSI)/American Dental Association (ADA) specification no. 57/2000 [18] (modified adoption of ISO 6876:2000) (Used for endodontic sealing materials) | Same as above | Same as above | Same as above |
| ISO 4049:2009 [19] (Used for polymer-based restorative materials) | Solubility: Samples immersed in water for 7 d are subsequently dehydrated to a constant mass. Solubility is given as the mass difference expressed as a function of specimen volume. Water sorption: Gain in mass of specimens following immersion in water for 7 d (recorded as a function of the specimen volume) | Water sorption and solubility values should not exceed 40 μg/mm3 and 7.5 μg/mm3, respectively | Cylindrical specimens, 1.5 mm ± 0.1 mm thickness, 1.0 ± 0.1 mm depth, and 15 mm internal diameter Samples immersed in distilled water for 7 d |

Table SII. Different terminologies have been used in the literature, often interchangeably, to explain the loss or removal of sealers when in contact with a fluid. The broader term “dissolution” should ideally be used.

| Terminology | Explanation |
| --- | --- |
| Solubility | Loss of mass during a period of immersion in water [84]. It is calculated as maximum percentage mass loss following immersion. |
| Water sorption | Calculated as maximum percent mass gain following immersion expressed as percentage increase in wet mass in comparison to original mass [39]. |
| Net water uptake | The sum of apparent water sorption and solubility since these processes are simultaneous [39]. |
| Disintegration | Differentiation between solubility and disintegration is difficult. There is liberation of particles from the material that remains in suspension, but the solvent remains clear [77]. |
| Dissolution | Process of making something slowly end or disappear |