Data is visually represented in the paper and more details are available on the tables in this supplement. Part of the results of this study were shared at the Academy of Dental Materials meeting in Porto de Galinhas, Brazil held on October 2018 [23].

Data for shear bond strength to enamel and dentine is presented in Table S1.

Wall-to-wall contraction obtained before and after thermocycling as well as after storage for 28 days is shown in Table S2.

Table S1 - Median and interquartile range (in parentheses) for shear bond strength (MPa) to enamel and dentine.

| Pretreatment | Restorative material | Bond strength (MPa) Enamel | Bond strength (MPa) Dentine |
| --- | --- | --- | --- |
| None | ACTIVA BioACTIVE Restorative | ** | ** |
|  | Fuji II LC | 13.9 (8.3)c p = 0.028 | 7.2 (9.9)c p = 0.002 |
| Etching | ACTIVA BioACTIVE Restorative | 30.9 (9.3)a p = 0.001 | ** |
|  | Fuji II LC | 24.0 (3.9)a p = 0.013 | 12.9 (7.1)b p = 0.004 |
| Adhesive | ACTIVA BioACTIVE Restorative | 19.3 (6.1)b p = 1.000 | 23.7 (17.8)a p = 0.657 |
|  | Ceram X Mono (control) | 18.1 (7.4)b | 19.0 (8.2)a |

** Not possible to measure due to loss of restorations. Superscript letters indicate significant differences among groups within each column. Significance (p values, 2-tailed) in the table results from Mann-Whitney U comparisons of each group with the control group (Ceram X Mono placed with self-etch adhesive Xeno Select).

Table S2 - Median and interquartile range (in parentheses) for wall-to-wall contraction (%) to cavities with margins in enamel and dentine.

|  |  | Before thermocycling |  | After thermocycling |  | After 28 days |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Pretreatment | Restorative material | Wall-to-wall contraction (%) Enamel | Wall-to-wall contraction (%) Dentine | Wall-to-wall contraction (%) Enamel | Wall-to-wall contraction (%) Dentine | Wall-to-wall contraction (%) Enamel | Wall-to-wall contraction (%) Dentine |
| None | ACTIVA BioACTIVE Restorative | 0.3 (0.2)bA p = 0.212 | 0.4 (0.4)b p = 0.039 | 0.4 (0.2)bA p = 0.940 | ** | 0.3 (0.1)cdA p = 0.103 | ** |
|  | Fuji II LC | 0.6 (0.5)bC p = 0.112 | 0.2 (0.3)aZ p = 0.139 | 0.3 (0.4)bB p = 0.289 | 0.1 (0.2)aY p = 0.056 | 0.1 (0.2)abA p = 0.05 | 0.0 (0.2)aY p = 0.314 |
| Etching | ACTIVA BioACTIVE Restorative | 0.0 (0.0)aA p < 0.001 | 0.4 (0.2)bY p = 0.001 | 0.2 (0.2)bB p = 0.075 | 0.6 (0.3)bYZ p = 0.002 | 0.3 (0.1)cB p = 0.424 | 0.5 (0.2)bZ p = 0.001 |
|  | Fuji II LC | 0.5 (0.4)bC p = 0.241 | 0.1 (0.2)aY p = 0.333 | 0.2 (0.3)aB p = 0.007 | 0.2 (0.2)aY p = 1.00 | 0.0 (0.0)aA p = 0.002 | 0.1 (0.2)aY p = 0.286 |
| Adhesive | ACTIVA BioACTIVE Restorative | 0.2 (0.1)aA p = 0.001 | 0.0 (0.4)aY p = 0.634 | 0.4 (0.2)bB p = 0.705 | 0.2 (0.1)aZ p = 0.743 | 0.4 (0.2)dB p = 0.033 | 0.1 (0.1)aYZ p = 0.379 |
|  | Ceram X Mono (control) | 0.5 (0.3)bB | 0.2 (0.3)aYZ | 0.4 (0.2)bB | 0.2 (0.1)aZ | 0.2 (0.2)bcA | 0.1 (0.1)aY |

1 out of 10 specimens from this group was lost;  3 out of 10 specimens from this group were lost;  6 out of 10 specimens from this group were lost. Superscript lowercase letters indicate significant differences among groups within each column. Significance (p values, 2-tailed) in the table results from Mann-Whitney U comparisons of each group with the control group (Ceram X Mono placed with self-etch adhesive Xeno Select). Superscript uppercase letters indicate significant differences within each line, i.e. within the same group at different moments of investigation. Here, letters from the beginning of the alphabet were used for comparisons of enamel data while letters from the end of the alphabet were used for comparisons of dentine data.